|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| |  |  | | --- | --- | |  |  | |  | |  | | --- | |  | |  | |  | |  | |  | |  | |  | |  | |  | |  | |  | | | |  |  |  |  | | --- | --- | --- | --- | |  |  |  |  | |  |  | |  | |  | | | | |  | | Databook (Log)  3-16-01  Gathered Scale, Mortar, Pipettes and graduated cylinder  Purchased Acetone   Produced first batch of TiO2 solution.  But went downhill when dish soap was added, turned to very dry paste.  Repeat above but didn't add much soap at all, and didn't mash again, also used more water   Lemon Leafs collected  Add acetone and mashed then filtered into plastic cup.  Plastic cup bad idea, as soon as I noticed the cup starting to dissolve, I placed it into a second cup and ran around franticly looking for a glass container, then washed it. I picked up the plastic cup to poor it into the glass cup, and well the bottom fell out, spilling acetone and chlorophyll everywhere! I immediately unplugged everything and aired out the area with a fan.  Repeated the Lemon Leaf to Chlorophyll procedure but didn't use plastic.  Repeated the same procedure for freshly mowed grass.  Collected Chromographs    3-17-01  TiO2 paste too wet, so I placed it in the sun to try to let some evaporate.  Forgot glass stirring rod, so I tried a smooth pen, that didn't work. Searched around stores and found a Martini mixing rod. Problem was it wasn't straight. But I managed after much frustration to perfect the TiO2 depositing. One hit was to quickly turn the dropper bottle upside down, so the drop of TiO2 wasn't bubbly.  First I tried just one TiO2 plate and the graphite pencil for the counter electrode.  They seemed good, so I wiped them clean, and start them over with the rest.   Used a candle to produce soot (carbon) layer on the counter electrode.  Began cooking glass slides on BBQ on top of aluminum foil, on high. 30 minutes latter turned off BBQ and allowed the plates to cool.   Placed slides into chlorophyll dye bottles  Began Dye process at 4:12 PM 3-17-01    3-18-01  Got raspberries and blackberries.   Mix 5 ml of water with the berries and a drop of acetone.  Crushed them, then filtered into lightproof containers.  Placed one TiO2 coated glass slide into each   15 minutes later remove them and wiped clean with alcohol.  Clamped Carbon coated side on them and place 1 drop of iodide on each side.  (Run #1 4:10pm 3-18-2001 Clear Skies)(second set reflects results after about 5 minutes of direct sun)        3-19-01  Resooted counter electrodes (didn't cook on BBQ)  Assembled cells, injected iodide then most of the soot broke upon iodide injection, sounds like the cooking does make a difference!  Weather haze and low sun, and bad cells, but still tried test, found cells very faulty as the removal of one binder clip would DRAMATICLY increase the output.  Cleaned all glass slides, resoot counter electrode, and recooked them on the BBQ.  Let them cool then placed them in there proper dye, rotating them to help eliminate errors.        3-20-01  Assembled cells and tested again. Sun decide to go behind some clouds and lower results, also TiO2 plates are starting to have too much carbon on them. The sun was low and covered which reduced results also.  Decided to go with Grass and blackberries.     3-21-01  Clean TiO2 and counter electrode plates, redid the TiO2 plate and used a pencil for the counter electrode this time. Ran all plates on BBQ for 20 minutes, only one burner on high, this didn't work    3-22-01  Reran glass plates on BBQ 25 minutes both burners on high, it worked this time. Made new grass and blackberry extracts, two of each. Places plates in them, hope to with good sun to be able to test them tomorrow.    3-24-01  Collected data on cells. Data looked good.    3-25-01  Collected data on cells, wiped slides clean, redeposited TiO2, BBQ for 25 minutes on high.    3-26-01  Collected data on cells, excellent data. | |  |  |  | | --- | --- | |  |  | |  | [[Electrifying The Sun](http://laflash.com/~chris/apbio/index.html)] [[Introduction](http://laflash.com/~chris/apbio/Introduction/introduction.html)] [[Hypothesis](http://laflash.com/~chris/apbio/Hypothesis/hypothesis.html)] [[Experiment](http://laflash.com/~chris/apbio/info/info.html)] [[Pictures](http://laflash.com/~chris/apbio/Pictures/pictures.html)] [[Data](http://laflash.com/~chris/apbio/data/data.html)] [[Conclusion](http://laflash.com/~chris/apbio/Conclusion/conclusion.html)] [[Recommendations](http://laflash.com/~chris/apbio/Recommendations/recommendations.html)] [[Bibliography](http://laflash.com/~chris/apbio/Bibliography/bibliography.html)] [[Experiment Log](http://laflash.com/~chris/apbio/Experiment_Log/experiment_log.html)] [[Acknowledgments](http://laflash.com/~chris/apbio/Acknowledgments/acknowledgments.html)] | |